## Slide 1: RHINO: Radiation Hardened robotics for remote INspectiOn
10 October 2024
Dr Saed Alrawash
Lancaster University

## Slide 2: Content
Work Plan Review
Diamond detector response
Future Work

## Slide 3: Project Overview (RHINO)
RHINO is pioneering a new generation of radiation-resistant robots:
  Simplified, robust design focused on surviving extreme environments, not just performing complex tasks
  Equipped with diamond-based radiation detector for real-time radiation monitoring as the robot navigates radioactive zone
What makes RHINO different?
  Continuous radiation tracking allows RHINO to retreat from dangerous areas before reaching critical damage
  Designed to operate in highly radioactive areas like Fukushima melted core

## Slide 4: My Role in the RHINO project
Focus on Neutron Detection
  Developing a diamond detector specifically for neutron radiation monitoring
Collaboration:
  Working with experts in robotics from University of Manchester, and electronics from Okayama University

## Slide 5: Overview
It is difficult to confirm the distribution of the fuel debris using γ-rays detection due to contamination of 137Cs.
Possible ways:
  γ-rays unique to fuel debris by using sensor has high energy resolution, comes from actinides that emits >1MeV
  other way: detect the spontaneous neutrons fission(mainly from 244Cm (98%))
  hence we chose neutron detector

## Slide 6: Work Plan Overview
Unknown fuel debris composition
Diamond detector response
Data acquisition system
Trained Machine Learning algorithm
Fuel material Identification
Monte Carlo Simulations
Real-World Data Collection
Machine Learning Training

## Slide 7: Why Choose Diamond Detector
1
Radiation-resistance
2
High-temperature resistance
3
Small size
4
High energy resolution
4
Fast response neutron detection
4
Gamma rejection

## Slide 8: Lancaster diamond detector
Thermal-Neutron Diamond Detector
Substrate material | sCVD diamond
Substrate thickness | 500 µm
Active area: | diameter 3 mm
Thermal neutron converter | 6Li(95% enriched)
Sensor size: | 4.5 mm x 4.5 mm
Nominal bias voltage: | 120 V
Housing size | 44 mm x 47 mm x 5 mm
developed for efficient thermal-neutron flux monitoring
high neutron detection rates up to 1 MHz
www.cividec.at

## Slide 9: Measurement setup
The detector current pulse has 7.2 ns FWHM, and the amplitude of 75 mV
Calibration done at the manufacturer with alpha particle of 5 MeV
Calibration with thermal neutrons with clear peaks of the alpha and He

## Slide 10: LU Diamond Detector Set up

## Slide 11: LU Diamond Detector Set up
Hamamatsu c10940-53

## Slide 12: Rectangular signal (Charged particle)
20 mV/div
5.00 ns/div
4 GS/s

## Slide 13: Triangular Signal (γ)

## Slide 14: External potential facilities
NILE Facility:
  Mixed flux of fast and thermal neutrons.
  Neutron flux achievable: Up to 10^6 n/s/cm^2.
EMMA Thermal Neutron Beamline:
  Thermal neutron flux of around 10^6 n/s/cm^2.
  Neutron energy selection possible with time of flight.
ChipIR Facility:
  Neutron energy may be too high for the experiment.
  Fast neutron flux saturation potential.
To understand the detector response for different neutron energies
NPL
IJS - Jozef Stefan Institute

## Slide 15: Geant4 MC Simulation
Neutron Source Cf252
Shielding material mix(ZrO2, Concrete, SS)
Diamond detector
Shielding material with different thicknesses
Mao, R., Zhang, L., & Zhu, R.-Y. (2023). "Fast Neutron Induced Nuclear Counter Effect in Hamamatsu Silicon PIN Diodes and APDs."
Cf252 neutron energy spectrum
acceptable tolerance for the bias voltage can be within ±5%. This means the voltage supply can range between 380 volts and 420 volts without significantly affecting the detector's performance

## Slide 16: Simulated Cf252 spectrum
Neutron energy spectrum of simulated Cf252 neutron source

## Slide 17: Energy deposition Vs Shielding
Shielding cm | Total Energy(MeV) | Number of Entries | Efficiency %
0 | 1346.995238 | 5617 | 0.5617
0.2 | 1300.465158 | 5369 | 0.5369
0.4 | 1254.038431 | 5084 | 0.5084
0.6 | 1222.0629 | 4757 | 0.4757
0.8 | 1119.260467 | 4416 | 0.4416
1 | 1087.070928 | 4294 | 0.4294
1.2 | 1044.603005 | 3958 | 0.3958
1.4 | 1010.694286 | 3821 | 0.3821
1.6 | 960.731924 | 3646 | 0.3646
1.8 | 901.1170527 | 3424 | 0.3424
2 | 859.9461396 | 3257 | 0.3257
2.2 | 865.1586714 | 3110 | 0.311
2.4 | 796.1386534 | 2957 | 0.2957
2.6 | 742.9587906 | 2793 | 0.2793
2.8 | 766.2246952 | 2694 | 0.2694
3 | 697.9863063 | 2522 | 0.2522
3.2 | 696.1249284 | 2432 | 0.2432
3.4 | 649.0340454 | 2286 | 0.2286
3.6 | 604.8060927 | 2164 | 0.2164
3.8 | 584.5151639 | 2095 | 0.2095
4 | 559.4185682 | 1969 | 0.1969
4.2 | 512.631663 | 1775 | 0.1775
4.4 | 504.3720303 | 1767 | 0.1767
4.6 | 508.9169485 | 1750 | 0.175
4.8 | 454.2168208 | 1562 | 0.1562
5 | 415.7863086 | 1475 | 0.1475

## Slide 18: Number of Interactions Vs Shielding
Shielding cm | Total Energy(MeV) | Number of Entries | Efficiency %
0 | 1346.995238 | 5617 | 0.5617
0.2 | 1300.465158 | 5369 | 0.5369
0.4 | 1254.038431 | 5084 | 0.5084
0.6 | 1222.0629 | 4757 | 0.4757
0.8 | 1119.260467 | 4416 | 0.4416
1 | 1087.070928 | 4294 | 0.4294
1.2 | 1044.603005 | 3958 | 0.3958
1.4 | 1010.694286 | 3821 | 0.3821
1.6 | 960.731924 | 3646 | 0.3646
1.8 | 901.1170527 | 3424 | 0.3424
2 | 859.9461396 | 3257 | 0.3257
2.2 | 865.1586714 | 3110 | 0.311
2.4 | 796.1386534 | 2957 | 0.2957
2.6 | 742.9587906 | 2793 | 0.2793
2.8 | 766.2246952 | 2694 | 0.2694
3 | 697.9863063 | 2522 | 0.2522
3.2 | 696.1249284 | 2432 | 0.2432
3.4 | 649.0340454 | 2286 | 0.2286
3.6 | 604.8060927 | 2164 | 0.2164
3.8 | 584.5151639 | 2095 | 0.2095
4 | 559.4185682 | 1969 | 0.1969
4.2 | 512.631663 | 1775 | 0.1775
4.4 | 504.3720303 | 1767 | 0.1767
4.6 | 508.9169485 | 1750 | 0.175
4.8 | 454.2168208 | 1562 | 0.1562
5 | 415.7863086 | 1475 | 0.1475

## Slide 19: Simulation of 226Ra Gamma Energy Spectrum
Fig.2 Real 226Ra gamma spectrum https://www.gammaspectacular.com/blue/ra226-spectrum
Energy (MeV)
Fig.1. Geant4 simulation results for 226Ra gamma source at Lancaster University Lab
Possible beta decay particles

## Slide 20: Secondary Particles in the Diamond
Number of secondary particles decreases with increasing shielding thickness
Shielding thickness increases
Knowledge of number of secondary particles with different thickness indicate the location of neutron source

## Slide 21: Experimental Results with Gamma sources
Exposed the detector at Lancaster University to gamma sources such as 137Cs, 60Co, 152Eu
Spectra were not as they supposed to be, diamond thickness is too small 500µm gamma passes through without interaction.
Advantages: Potential benefits for gamma rejection in mixed radiation environments

## Slide 22: Detector setup
Detector
Amplifier
HV
MCA
On the robot
Off the robot
HV> Cable could be extended to 100m if high quality cable is used (1.6 kg/100 m)
MCA for high accuracy count rate
+400 V
12 V
5 V

## Slide 23: Machine Learning Model
Nuclides Inventory (JAEA, ORIGEN2)
Neutron emission rate emission rate
Weight
Corium thickness
Pedestal
Python
Detector Response
Total Energy Deposition
Count rate
Results 1800 files
Python: data extraction
Machine Learning Dataset
MATLAB Regression Learner models
Material | MELCOR | MAAP | MCNPX
UO2 | 69.4 | 76.15 | 75.77
Zr | 25.8 | 16.59 | 17.8
ZrO2 | 16.6 | 14.14 | 13.82
B4C | 0 | 0.502 | 0.59
Cr | 5.9 | 1.13 | 1.1
Cr2O3 | 0.03 | 2.732 | 2.73
FeO | 0.23 | 11.2 | 11.2
Ni | 2.53 | 0.55 | 0.556
NiO | 0.03 | 1.2 | 1.2
Table 1. Corium mixture components inventory at the time of accident in tons.

## Slide 24: Future work
Simulation results for the neutron count rate
Comparison between Simulation and experimental data
Monoenergetic neutron exposure produced by Van de Graaff accelerator, NPL.

## Slide 25: Thank you for attending, any questions?

## Slide 26: Response to Matt questions
Are we trying to detect the material directly below the robot? Yes, we need no materials in between the detector the corium.
Cable selection?
For the 400V I assume that is very low current? Do you know if it needs to be well regulated.
    Low current, 75mA.
    Yes it is important keep a regulated voltage to ensure consistent and accurate performance

## Slide 27: Diamond Vs Silicon Carbide
The count rate of the diamond-based detector has been higher than the count rate of the SiC-based detector.
  This fact is due to the smaller thickness of the active detection volume of the SiC-based detector which is limited to 21 μm.
Better gamma rejection of Diamond to that of SiC
PKA in diamond will create fewer atomic displacements than SiC
parameter | SiC | Diamond
Electron mobility(cm2/Vs) | 1000 | 2000
displacement energy (eV) | 20-30 | 40-50
DPA(x10E-20) (under 1MeV neutron flux) | 4.12 | 1.30
Average PKA energy(keV) under 1MeV neutron flux | 73.68 | 134.30
DPA: displacement per atom
PKA: primary knock-on atom
Z. Zhang and M. D. Aspinal, “Comparison of neutron detection performance of four thin-film semiconductor neutron detectors based on geant4,” Sensors, vol. 21, no. 23, 2021, doi: 10.3390/s21237930.

## Slide 28: Diamond Vs Silicon Carbide
Experiment done MINERVE facility at CEA Cadarache.
  The experiment show that diamond has higher gamma rejection, as well as higher detection efficiency.
  It also shows that the diamond has a better signal-to-noise ratio than the SiC
O. Obraztsova et al., “Comparison between Silicon Carbide and Diamond for Thermal Neutron Detection at Room Temperature,” IEEE Trans. Nucl. Sci., vol. 67, no. 5, pp. 863–871, 2020, doi: 10.1109/TNS.2020.2981059
In the same experiment: it Was observed the diamond reaction peak shifting and count rate reduction after 600s of neutron irradiation
The same effect was noticed for the semi-insulating SiC detectors but not for the epitaxial SiC detectors
This effect could be minimized by the reduction of the diamond thickness and by the increase in the applied bias voltage

## Slide 29: Experimental evidence of radiation hardness of Diamond-based sensor
Some experiment reported that for a 25 µm thick diamond no effects are visible up to a 14 MeV neutron effluence of 2x1014 n/cm2
Whereas in another experiment after a effluence of 2x1016 n/cm2, the 25 µm thick diamond showed a severe degradation in efficiency and energy resolution, from 100% to 47% and from 1.4% to 10.3%, respectively
Pillon, M.; etl. Radiation tolerance of a high quality synthetic single crystal chemical vapor deposition diamond detector irradiated by 14.8 MeV neutrons. J. Appl. Phys. 2008, 104, 054513
Almaviva, etl. Characterization of damage induced by heavy neutron irradiation on multilayered L6iF-single crystal chemical vapor deposition
diamond detectors. J. Appl. Phys. 2009
Neutron effluence inside Fukushima melted core is ~ 1009

## Slide 30: Experimental evidence of radiation hardness of Diamond-based sensor
Few experimental data are available in the literature for gamma exposure
One experiment where diamond exposed to a high dose up to 5MGy of 60Co Energy-gamma=1250keV, showed a damage to the metal contact
Grácio, J.; Fan, Q.H.; Madaleno, J.C. Diamond growth by chemical vapour deposition. J. Phys. D Appl. Phys. 2010
Inside the melted core radiation intensity could reach 1000 Gy/h
The pressure vessel is flooded with water which acts as a radiation shield. Is the robot submerged?
However